# Heat of Hydration of Portland and Composite Cements Under Semi-Adiabatic Conditions

# ABSTRACT:

Heat generated during cement hydration is a critical factor influencing temperature rise and the risk of thermal cracking in mass concrete structures. Reliable prediction of early-age temperature development requires accurate characterization of hydration kinetics for commonly used cement types under controlled conditions. This study investigates the hydration behavior of four commercially available cements conforming to BDS EN 197-1:2003: CEM I 52.5N, CEM II A-M 42.5N, CEM II A-M 42.5R, and CEM II B-M 42.5N, tested under semi-adiabatic and sealed conditions. The inclusion of the rapid-hardening variant CEM II A-M 42.5R alongside its standard-strength counterpart enables a direct assessment of how early strength gain characteristics influence overall hydration heat evolution.

Mineralogical characterization was performed using X-ray diffraction (XRD) to identify major clinker phases, including C₃S, C₂S, C₃A, and C₄AF. Hydration heat evolution was monitored by semi-adiabatic calorimetry, from which the heat generation rate and cumulative heat release were determined for each cement type. A MATLAB-based two-component Gaussian model was applied to represent the multi-stage hydration process by separately capturing the early aluminate reaction and the dominant silicate hydration peak. In addition, cumulative heat evolution was modeled using sixth-order polynomial functions to produce continuous analytical expressions suitable for numerical thermal simulations. Experimental observations were further validated using hydration predictions from the NIST Virtual Cement and Concrete Testing Laboratory (VCCTL).

Results show clear differences in thermal behavior among the four tested cements. CEM I 52.5N exhibited the highest cumulative heat release (~500 J/g) and the fastest overall hydration kinetics, indicating the greatest thermal cracking potential in mass concrete applications. CEM II A-M 42.5R demonstrated notably accelerated early-age heat evolution relative to the standard CEM II A-M 42.5N, reflecting its higher reactive phase content and finer grinding, though its long-term cumulative heat remained moderate. CEM II A-M 42.5N showed intermediate thermal behavior between the high-heat and low-heat cement. In contrast, CEM II B-M 42.5N exhibited the lowest cumulative heat release (~300 J/g) and the slowest heat evolution, suggesting the most favorable thermal performance for temperature-sensitive concrete placements.

The developed hydration models provide practical input parameters for thermal analysis, cement selection, and temperature-control strategies in mass concrete structures, with particular emphasis on distinguishing the role of rapid-hardening cements in early-age thermal risk assessment.

Keywords: Heat of hydration; mass concrete; semi-adiabatic calorimetry; XRD; Gaussian modeling; MATLAB; VCCTL; thermal cracking.