This is the simple example template containing only headers for each report item and the bookmarks. The invisible bookmarks are indicated by text between brackets.

Modify it according to your own needs and standards.

## Measurement Conditions:  (Bookmark 1)

Dataset Name	3

File name	E:\XRD data files\Monira\Adhoc\2026\buet civil\3.xrdml

Comment	Configuration=Flat Sample Stage, Owner=pc, Creation date=11/22/2023 7:32:59 PM

Goniometer=Theta/Theta; Minimum step size 2Theta:0.0001; Minimum step size Omega:0.0001

Sample stage=Stage for flat samples/holders

Diffractometer system=EMPYREAN

Measurement program=C:\PANalytical\Data Collector\Programs\Fiber.xrdmp, Created identifier={E8C07BD7-8A8C-42E2-8622-4BC130302805}, Created by=pc, Id=WL:DESKTOP-BC0RBBD:pc, Creation date=1/6/2025 4:49:46 PM, Modified identifier={32F7A4C4-C999-46E4-852F-B36327219E96}, Modified by=pc, Id=WL:DESKTOP-BC0RBBD:pc, Modification date=1/12/2026 4:17:19 PM

PHD Lower Level = 7.89 (keV), PHD Upper Level = 11.27 (keV)

Measurement Start Date/Time	2/17/2026 1:01:10 PM

Operator	pc

Raw Data Origin	XRD measurement (*.XRDML)

Scan Axis	Gonio

Start Position [°2θ]	6.0056

End Position [°2θ]	89.9856

Step Size [°2θ]	0.0260

Scan Step Time [s]	7.1400

Scan Type	Continuous

PSD Mode	Scanning

PSD Length [°2θ]	3.35

Offset [°2θ]	0.0000

Divergence Slit Type	Fixed

Divergence Slit Size [°]	0.7197

Specimen Length [mm]	10.00

Measurement Temperature [°C]	25.00

Anode Material	Cu

Intended Wavelength Type	K-α1

K-α1 [Å]	1.54060

K-α2 [Å]	1.54443

K-β1 [Å]	1.39225

K-β2 [Å]	1.38113

K-β3 [Å]	1.39261

K-A2 / K-A1 Ratio	0.50000

K-Alpha2 Line Shift	0.00000

K Absorption Edge	1.37868

Generator Settings	40 mA, 45 kV

Diffractometer Type	0000000011286122

Diffractometer Number	0

Goniometer Radius [mm]	240.00

Dist. Focus-Diverg. Slit [mm]	60.50

Incident Beam Monochromator	No

Spinning	No

## Main Graphics, Analyze View: (Bookmark 2)

## Peak List: (Bookmark 3)

| Pos. [°2θ] | Height [cts] | FWHM Left [°2θ] | d-spacing [Å] | Rel. Int. [%] |
| --- | --- | --- | --- | --- |
| 11.7424 | 77.65 | 0.1791 | 7.53035 | 11.71 |
| 20.8432 | 53.29 | 0.1535 | 4.25839 | 8.04 |
| 23.1278 | 43.90 | 0.2558 | 3.84264 | 6.62 |
| 26.7102 | 61.58 | 0.1023 | 3.33484 | 9.29 |
| 29.5361 | 663.00 | 0.1535 | 3.02189 | 100.00 |
| 30.2677 | 74.15 | 0.1791 | 2.95049 | 11.18 |
| 31.1356 | 24.76 | 0.3070 | 2.87020 | 3.73 |
| 32.3493 | 514.04 | 0.1023 | 2.76523 | 77.53 |
| 32.7670 | 304.45 | 0.2047 | 2.73093 | 45.92 |
| 33.3648 | 101.58 | 0.1535 | 2.68335 | 15.32 |
| 33.9923 | 86.97 | 0.2047 | 2.63524 | 13.12 |
| 34.5061 | 421.10 | 0.1535 | 2.59717 | 63.51 |
| 36.1214 | 63.44 | 0.1279 | 2.48464 | 9.57 |
| 36.8586 | 56.68 | 0.1535 | 2.43662 | 8.55 |
| 38.8881 | 61.17 | 0.1535 | 2.31400 | 9.23 |
| 39.5965 | 84.58 | 0.1791 | 2.27422 | 12.76 |
| 41.4617 | 214.12 | 0.2047 | 2.17612 | 32.30 |
| 43.3387 | 63.05 | 0.1535 | 2.08612 | 9.51 |
| 45.9557 | 27.99 | 0.2558 | 1.97323 | 4.22 |
| 47.0863 | 56.05 | 0.1535 | 1.92845 | 8.45 |
| 47.6494 | 89.87 | 0.1023 | 1.90696 | 13.55 |
| 48.6748 | 66.29 | 0.1535 | 1.86916 | 10.00 |
| 50.0699 | 26.28 | 0.4093 | 1.82030 | 3.96 |
| 51.8945 | 170.56 | 0.3070 | 1.76051 | 25.73 |
| 56.6844 | 92.90 | 0.2558 | 1.62258 | 14.01 |
| 57.5672 | 29.41 | 0.2047 | 1.59978 | 4.44 |
| 60.0969 | 81.81 | 0.1023 | 1.53835 | 12.34 |
| 62.3900 | 86.63 | 0.2558 | 1.48720 | 13.07 |
| 63.8728 | 28.69 | 0.2558 | 1.45620 | 4.33 |
| 67.6269 | 12.71 | 0.4093 | 1.38421 | 1.92 |
| 79.7825 | 7.41 | 1.2280 | 1.20109 | 1.12 |
| 83.7337 | 9.39 | 0.6140 | 1.15418 | 1.42 |
| 85.7120 | 11.68 | 0.5117 | 1.13253 | 1.76 |

## Pattern List: (Bookmark 4)

| Visible | Ref.Code | Score | Compound Name | Displ.[°2θ] | Scale Fac. | Chem. Formula |
| --- | --- | --- | --- | --- | --- | --- |
| * | 00-042-0551 | 61 | Calcium Silicate | 0.000 | 0.596 | Ca3 Si O5 |
| * | 01-072-4582 | 49 | Calcium Carbonate | 0.000 | 0.525 | Ca ( C O3 ) |
| * | 01-085-0865 | 16 | Silicon Oxide | 0.000 | 0.064 | Si O2 |
| * | 01-080-2797 | 17 | Calcium Carbonate | 0.000 | 0.146 | Ca ( C O3 ) |
| * | 01-083-2208 | 15 | Calcium Aluminum Silicate | 0.000 | 0.136 | Ca3 Al2 Si3 O12 |
| * | 01-073-2091 | 18 | Calcium Silicate | 0.000 | 0.298 | Ca2 ( Si O4 ) |

## Document History: (Bookmark 5)

ESD calculated from counts:

- Modification time = "2/17/2026 4:31:38 PM"

- Modification editor = "pc"

Insert Measurement:

- File name = "3.xrdml"

- Modification time = "2/17/2026 4:31:38 PM"

- Modification editor = "pc"

Default properties:

- Measurement step axis = "None"

- Internal wavelengths used from anode material: Copper (Cu)

- Original K-Alpha1 wavelength = "1.54060"

- Used K-Alpha1 wavelength = "1.54060"

- Original K-Alpha2 wavelength = "1.54443"

- Used K-Alpha2 wavelength = "1.54443"

- Original K-Beta wavelength = "1.39225"

- Used K-Beta wavelength = "1.39225"

- Irradiated length = "10.00000"

- Spinner used = "No"

- KBeta filter material = "Ni"

- KBeta filter thickness = "0.02000"

- Receiving slit size = "0.10000"

- Step axis value = "0.00000"

- Offset = "0.00000"

- Sample length = "10.00000"

- Modification time = "2/17/2026 4:31:38 PM"

- Modification editor = "pc"

Interpolate Step Size:

- Initial Scan Range = 6.00563 - 89.98690

- Initial Step Size = 0.02626

- Derived Step Size = 0.02600

- Use Derived Step Size = "Yes"

- Parameterset name = "Default"

- PANalytical factory default

- Modification time = "2/17/2026 4:31:38 PM"

- Modification editor = "pc"

Determine Background:

- Add to net scan = "Nothing"

- User defined intensity = "-5"

- Correction method = "Automatic"

- Bending factor = "3"

- Minimum significance = "0.7"

- Minimum tip width = "0"

- Maximum tip width = "1"

- Peak base width = "2"

- Use smoothed input data = "Yes"

- Granularity = "24"

- Search window = "5"

- Spline type = "Linear"

- Parameterset name = "Untitled"

- Parameterset modification time = "2/17/2026 12:34:33 PM"

- Parameterset modification editor = "pc"

- Modification time = "2/17/2026 4:32:00 PM"

- Modification editor = "pc"

Search Peaks:

- Minimum significance = "1"

- Minimum tip width = "0.1"

- Maximum tip width = "1.8"

- Peak base width = "2"

- Method = "Minimum 2nd derivative"

- Parameterset name = "Untitled"

- Parameterset modification time = "2/17/2026 12:38:53 PM"

- Parameterset modification editor = "pc"

- Modification time = "2/17/2026 4:32:05 PM"

- Modification editor = "pc"

Search & Match:

- Allow pattern shift = "No"

- Auto residue = "Yes"

- Data source = "Profile and peak list"

- Demote unmatched strong = "Yes"

- Multi phase = "Yes"

- Restriction set = "Untitled"

- Restriction = "Restriction set"

- Subset name = ""

- Match intensity = "Yes"

- Two theta shift = "0"

- Identify = "No"

- Max. no. of accepted patterns = "5"

- Minimum score = "50"

- Min. new lines / total lines = "60"

- Search depth = "10"

- Minimum new lines = "5"

- Minimum scale factor = "0.1"

- Intensity threshold = "0"

- Use line clustering = "Yes"

- Line cluster range = "1.5"

- Search sensitivity = "1.8"

- Use adaptive smoothing = "Yes"

- Smoothing range = "1.5"

- Threshold factor = "3"

- Match Threshold = "0"

- N * Esds = "-1"

- Raw Weight = "-1"

- Peak Shape = "-1"

- Accepted Shape = "-1"

- Peak Power = "-1"

- New Peak Power = "-1"

- Intensity Power = "-1"

- N Peaks Power = "-1"

- Parameterset name = "Untitled"

- Parameterset modification time = "2/17/2026 12:44:41 PM"

- Parameterset modification editor = "pc"

- Modification time = "2/17/2026 4:32:20 PM"

- Modification editor = "pc"

## XRD Measurement Information: (Bookmark 6)

More items… (Bookmark 7)

More items… (Bookmark 8)

More items… (Bookmark 9)

More items… (Bookmark 10)

More items… (Bookmark 11)

More items… (Bookmark 12)

More items… (Bookmark 13)

More items… (Bookmark 14)

More items… (Bookmark 15)