## Slide 1
BANGLADESH UNIVERSITY OF ENGINEERING AND TECHNOLOGY
Department of Civil Engineering
Heat of Hydration of
Portland and Composite Cements
Under Semi-Adiabatic Conditions
Zisan Zia
ID: 2004153
Abdur Nur Tushar
ID: 2004061
Supervisor: Dr. Raquib Ahsan, Professor, Dept. of Civil Engineering, BUET
1

## Slide 2
Portland vs. Composite Cement
P
Portland Cement — CEM I
High clinker content
Fast early hydration
Higher heat release
Useful for early strength gain
Clinker: High
Heat: High
C
Composite Cement — CEM II
Clinker partly replaced by SCM/filler
Slower heat evolution
Lower thermal cracking risk
Suitable for large mass pours
Replacing clinker generally reduces heat — but rapid-hardening composite cement can still spike early heat through increased fineness.
Zisan Zia • 2004153
Dept. of Civil Engineering, BUET
2004153
Clinker: Lower
Heat: Lower
2

## Slide 3
Reasons Behind Choosing Semi-Adiabatic Calorimetry
≈
Isothermal Calorimetry
T = constant (bath)
Keeps temperature constant
Very accurate for reaction kinetics
Requires specialized instrument
Small sample — not representative of field
vs
△
Semi-Adiabatic Calorimetry
T rises naturally (insulated vessel)
Allows limited, controlled heat loss
Temperature rises as in real concrete
Practical, low-cost, reproducible
Closest to field mass concrete behaviour
Real concrete is neither isothermal nor perfectly adiabatic — semi-adiabatic captures the practical heat-retention condition of mass placements.
Zisan Zia • 2004153
Dept. of Civil Engineering, BUET
2004153
3

## Slide 4
Reasons Behind Hydration Heat Calculation
1
Reaction Speed
q(t) shows how fast the cement reacts at each instant
2
Total Heat
Q(t) shows heat stored over time — drives temperature rise
3
Cracking Risk
High heat → high ΔT → thermal stress exceeding tensile strength
4
Cement Choice
Low-heat cement identified as suitable for mass concrete pours
Hydration heat parameters feed early-age thermal analysis, temperature-control planning, and cement selection for mass concrete.
Zisan Zia • 2004153
Dept. of Civil Engineering, BUET
2004153
4

## Slide 5
Research Gaps
BD
Bangladesh Cement Data Gap
Limited semi-adiabatic hydration heat data for BDS EN 197-1 cement types commonly used in Bangladeshi construction.
⚡
Early Heat Risk Gap
Rapid-hardening composite cement (CEM II A-M 42.5 R) produces faster early heat — this behaviour is rarely isolated from normal composite cement.
✓
Composite Cement Validation Gap
CEM II A-M and B-M with mixed secondary constituents lack systematic heat-evolution validation under semi-adiabatic conditions.
This study fills all three gaps: XRD + semi-adiabatic calorimetry + MATLAB modelling + VCCTL simulation
Zisan Zia • 2004153
Dept. of Civil Engineering, BUET
2004153
5

## Slide 6
Objectives and Scope
Objective 1 — Characterise & Measure
XRD phase identification (C₃S, C₂S, C₃A, CaCO₃, SCM)
Temperature development under sealed conditions
Heat generation rate q(t) and cumulative heat Q(t)
Objective 2 — Heat Modeling & Validation
Convert temperature rise into hydration heat release
Analyze heat emission rate and cumulative heat evolution
Model hydration peaks using MATLAB Gaussian fitting
Generate smooth polynomial heat functions for thermal simulation
Key Output Parameters
q(t)
Heat generation rate
Q(t)
Cumulative heat release
Peak time
Time to max heat rate
α(t)
Degree of hydration
Risk rank
Cement suitability
Zisan Zia • 2004153
Dept. of Civil Engineering, BUET
2004153
6

## Slide 7
Four Cement Samples Compared
CEM I
52.5 N
Portland
high clinker / high-heat reference
Heat Baseline
CEM II A-M
42.5 R
Composite, rapid
rapid-hardening spike early heat
Early-Heat Challenge
CEM II A-M
42.5 N
Composite, normal
intermediate heat control
Comparison Point
CEM II B-M
42.5 N
Higher composite
low-heat candidate for mass concrete
Low-Heat Target
Zisan Zia • 2004153
Dept. of Civil Engineering, BUET
2004153
7

## Slide 8
Research Workflow
1
Cement Selection
CEM I 52.5 N
CEM II A-M 42.5 R
CEM II A-M 42.5 N
CEM II B-M 42.5 N
2
Sample Prep
Sealed paste
w/c ≈ 0.40
3
XRD Testing
Identify C₃S, C₂S,
C₃A, CaCO₃, SCM
4
Calorimetry
Record Tₛ(t)
and Tₐₘᵦ(t)
5
Heat Calculation
q(t), Q(t)
and peak time
6
Model & Validate
Gaussian, polynomial,
VCCTL( Virtual Cement and Concrete Testing Laboratory)
Zisan Zia • 2004153
Dept. of Civil Engineering, BUET
2004153
8

## Slide 9
Sample Preparation and XRD Testing
01
Oven Dry
Remove moisture before XRD to avoid peak distortion
02
Grind Powder
Achieve fine, uniform particles for flat sample surface
03
Load Holder
Flat surface, minimise preferred orientation effects
04
Run XRD Scan
6°–90° 2θ with Cu Kα₁, step 0.026°, 7.14 s/step
05
Match Phases
HighScore Plus software + ICDD PDF database
Zisan Zia • 2004153
Dept. of Civil Engineering, BUET
2004153
powder sample
9

## Slide 10
XRD Measurement Conditions
Parameter | Value
Instrument | PANalytical EMPYREAN
Radiation | Cu Kα₁ = 1.54060 Å
Scan range | 6.006° – 89.986° 2θ
Step size | 0.0260° 2θ
Step time | 7.1400 s
Generator | 45 kV, 40 mA
Temperature | 25 °C
Zisan Zia • 2004153
Dept. of Civil Engineering, BUET
2004153
10

## Slide 11
CEM II B-M 42.5 N
XRD diffractograms: four samples
CEM II A-M 42.5 N
CEM II A-M 42.5 R
CEM I 52.5 N
2004153
11
Zisan Zia • 2004153
Dept. of Civil Engineering, BUET

## Slide 12
Semi-Quantitative XRD Phase Composition
Why rapid hardening shows high early heat
CEM II A-M 42.5R has a high reactive clinker fraction:
C₃S + C₂S + C₃A + C₄AF
= 51.5 + 14.6 + 7.8 + 7.8
= 81.7%
High C₃S gives faster early hydration and strength gain
C₃A increases early heat emission
Zisan Zia • 2004153
Dept. of Civil Engineering, BUET
2004153
12

## Slide 13
From Phase Composition to Heat Evolution
C₃S / Alite
Fast heat + early strength
C₂S / Belite
Slower, later-age hydration
C₃A / Aluminate
Early exothermic spike (1st peak)
CaCO₃ / Filler
Clinker dilution → reduces heat generation
Mixed Mineral Additions
Slower hydration + lowest cumulative heat
Zisan Zia • 2004153
Dept. of Civil Engineering, BUET
2004153
Zisan Zia • 2004153
Dept. of Civil Engineering, BUET
13

## Slide 14
High Reactive Clinker Fraction
C₃S
51.5%
C₂S
14.6%
C₃A
7.8%
C₄AF
7.8%
Filler
14.5%
Best For — Early Strength Applications
✓ Precast concrete — fast demoulding cycle
✓ Cold-weather pours — gain strength before freeze
✓ Rapid formwork removal in framed structures
✓ Road repairs needing early opening to traffic
CEM II A-M 42.5R
2004153
Zisan Zia • 2004153
Dept. of Civil Engineering, BUET
14

## Slide 15
Semi-Adiabatic Calorimetry Setup
14 / 22
2004153
Semi-Adiabatic Calorimetry Setup
2004153
instrumented setup
temperature logging
Instrumental Setup
15
Zisan Zia • 2004153
Dept. of Civil Engineering, BUET

## Slide 16
Semi-Adiabatic Calorimetry Setup
1
Sample Vial
Sealed cement paste (w/c=0.40) in polypropylene vial
2
Temperature Sensors
Thermocouples record Tₛ(t) sample and Tₐₘᵦ(t) ambient
3
Insulation
Limits — but does not eliminate — heat loss to surroundings
4
Data Logger + PC
Continuous temperature record at fixed time intervals
Zisan Zia • 2004153
Dept. of Civil Engineering, BUET
2004153
setup schematic
16

## Slide 17
Calorimeter Calibration
2004153
Zisan Zia • 2004153
Dept. of Civil Engineering, BUET
17

## Slide 18
Calorimeter Calibration
2004153
Zisan Zia • 2004153
Dept. of Civil Engineering, BUET
18

## Slide 19
Calorimeter Calibration
1
System capacity, C
3076.9 J/K
2
Insulator capacity
1386.6 J/K
3
Heat-loss coeff., Kᴸ
0.0356 W/K
How we calibrated
Electrical heating test → temperature rise → determine C
Cooling test → exponential decay → extract Kᴸ from T(t) curve
C and Kᴸ inserted into heat balance equation for all test runs
Zisan Zia • 2004153
Dept. of Civil Engineering, BUET
2004153
Cooling model
T(t) − Tₐₘᵦ = (T₀ − Tₐₘᵦ) · e^(−Kᴸt / C)
Uncertainty from calibration: ~±3%
19

## Slide 20
Heat Calculation Algorithm
Processing logic from raw temperature data to heat outputs
2004061
1
Clean &
Standardise
t → 0, 5, 10,… min
→ Ts(t), Tamb(t)
▶
2
Hydration
Degree
r(t) = Qv(t)
/ Qv,max
→ r(t) at each step
▶
3
Heat
Balance
q̇ = Ca·dT/dt
+ KL(Ts−Tamb)
→ Total heat flow q̇
▶
4
Specific
Heat Rate
qg(t) = q̇ / mc
→ Specific rate qg(t)
▶
5
Integrate
& Fit
Q(t) = ∫ qg(t)·dt
→ Cumulative heat Q(t)
Goal: convert T(t) measurements into qᵍ(t), Q(t), peak heat rate, and Gaussian fitting Curves for thermal simulation
Abdur Nur Tushar • 2004061
20
Dept. of Civil Engineering, BUET

## Slide 21
Variable Specific Heat of Hardening Cement Paste
Specific heat decreases linearly as hydration advances — De Schutter & Taerwe (1995)
Key Formula
Ca(r) = 1160.67 × (1.5 − 0.5·r)
J / kg · K
Adapted for CEM II A-M 42.5 R, w/c = 0.40
r = degree of hydration
(0 = fresh paste → 1 = fully hydrated)
Cₚ falls from ~1754 → ~1300 J/kg·K
as denser C-S-H gel replaces water
De Schutter and Taerwe (1995) established a relationship between the specific heat of cement paste and the degree of hydration
Abdur Nur Tushar • 2004061
Dept. of Civil Engineering, BUET
2004061
21

## Slide 22
Key Outputs and What They Mean
Parameters used for comparison and thermal risk assessment
Qg(t)
Specific Heat Generation Rate
The peak time and amplitude distinguish fast from slow cements.
Q(t)
Cumulative Heat Release
Higher Heat larger adiabatic ΔT and greater thermal cracking risk.
Peak time
Time to Maximum Heat Rate
Earlier peak means faster early reaction.
α(t)
Degree of Hydration
Mea (0→1). Used for VCCTL comparison and variable heat-capacity correction.
Risk rank
Cement Selection Output
Combines heat magnitude + timing → ranks cements for mass concrete use
Abdur Nur Tushar • 2004061
Dept. of Civil Engineering, BUET
2004061
22

## Slide 23
Result Detail: CEM I , CEM II A-M R, CEM II A-M N, CEM II B-M N
Goal: convert T(t) data into qᵍ(t), Q(t), peak heat rate, and model-ready fitting curves for thermal simulation.
Abdur Nur Tushar • 2004061
Dept. of Civil Engineering, BUET
High clinker content produces the strongest and fastest hydration heat response.
2004061
23

## Slide 24
Result Detail: CEM I , CEM II A-M R, CEM II A-M N, CEM II B-M N
Goal: convert T(t) data into qᵍ(t), Q(t), peak heat rate, and model-ready fitting curves for thermal simulation.
Abdur Nur Tushar • 2004061
Dept. of Civil Engineering, BUET
High clinker content produces the strongest and fastest hydration heat response.
Peak width
Tail behavior
Peak height
Peak time
Peak width
Tail behavior
2004061
24

## Slide 25
Result Detail: CEM I , CEM II A-M R, CEM II A-M N, CEM II B-M N
Goal: convert T(t) data into qᵍ(t), Q(t), peak heat rate, and model-ready fitting curves for thermal simulation.
Abdur Nur Tushar • 2004061
Dept. of Civil Engineering, BUET
High clinker content produces the strongest and fastest hydration heat response.
2004061
25

## Slide 26
Result Detail: CEM I , CEM II A-M R, CEM II A-M N, CEM II B-M N
Goal: convert T(t) data into qᵍ(t), Q(t), peak heat rate, and model-ready fitting curves for thermal simulation.
Abdur Nur Tushar • 2004061
Dept. of Civil Engineering, BUET
High clinker content produces the strongest and fastest hydration heat response.
Chart: 
| CEM I | A-M R | A-M N | B-M N
Cumulative heat | 467 | 433 | 270 | 250
Approximate final cumulative heat release
2004061
26

## Slide 27
Results: Cumulative Heat Release
Terminal Q at end of monitoring period — experimental vs. Gaussian model fit
Chart: 
| CEM I 52.5N | CEM II A-M 42.5R | CEM II A-M 42.5N | CEM II B-M 42.5N
Experimental (J/g) | 467 | 433 | 284 | 255
Gauss-2 Fit (J/g) | 438 | 447 | 262 | 242
Cumulative Heat Release (J/g)
CEM I 52.5 N: ~467 J/g — highest cumulative heat. Greatest thermal cracking risk (ΔT > 40°C adiabatic).
CEM II A-M 42.5 R: ~433 J/g — almost as high as Portland, driven by finer grinding and higher surface area.
CEM II A-M 42.5 N: ~284 J/g — intermediate; mineral additions dilute clinker and slow hydration.
CEM II B-M 42.5 N: ~255 J/g — lowest heat. Best choice for thermally sensitive mass concrete.
Abdur Nur Tushar • 2004061
Dept. of Civil Engineering, BUET
2004061
27

## Slide 28
VCCTL Hydration Simulation
Chart: 
| CEM I | A-M N | B-M N | A-M R
DOH at 19 h | 0.82 | 0.95 | 0.825 | 0.8
VCCTL-predicted degree of hydration at 19 h
DOH comparisons
Abdur Nur Tushar • 2004061
Dept. of Civil Engineering, BUET
2004061
28
Notes: Show the DOH values. Explain that isothermal VCCTL may differ in absolute numbers, but trend validation is the key.

## Slide 29
VCCTL heat release validation
Chart: 
| CEM I | A-M N | B-M N | A-M R
Heat release at 19 h | 480 | 390 | 348 | 480
VCCTL cumulative heat release at 19 h
CEM I
≈480 kJ/kg
A-M N
≈390 kJ/kg
B-M N
≈348 kJ/kg
A-M R
≈445 kJ/kg
Abdur Nur Tushar • 2004061
Dept. of Civil Engineering, BUET
2004061
29
Notes: Use this slide to connect validation with conclusions. The simulated values support the experimental interpretation.

## Slide 30
VCCTL Simulation and Validation
NIST VCCTL independently confirms the experimental heat rankings
Chart: 
| CEM I 52.5N | CEM II A-M 42.5R | CEM II A-M 42.5N | CEM II B-M 42.5N
Experimental Q (J/g) | 467 | 433 | 284 | 255
VCCTL predicted (kJ/kg) | 480 | 445 | 390 | 348
Heat release at 19h Experimental (J/g) vs VCCTL (kJ/kg) same relative scale
VCCTL Degree of Hydration at 19 h (isothermal)
Cement | DOH at 19h
CEM I 52.5 N | ≈ 0.80
CEM II A-M 42.5 R | ≈ 0.800
CEM II A-M 42.5 N | ≈ 0.950
CEM II B-M 42.5 N | ≈ 0.825
VCCTL systematically over-predicts composite cement heat (isothermal vs semi-adiabatic). Relative ranking is fully confirmed. Residual scatter within ±3% calibration uncertainty.
Abdur Nur Tushar • 2004061
Dept. of Civil Engineering, BUET
2004061
30

## Slide 31
Conclusions and Practical Implications
Thermal Cracking Risk Ranking
CEM I 52.5 N
~467 J/g
ΔT > 40°C
HIGHEST RISK
CEM II A-M 42.5 R
~433 J/g
ΔT 32–38°C
HIGH
CEM II A-M 42.5 N
~284 J/g
ΔT 25–28°C
MODERATE
CEM II B-M 42.5 N
~255 J/g
ΔT 22–25°C
LOWEST RISK
Abdur Nur Tushar • 2004061
Dept. of Civil Engineering, BUET
Key Findings
CEM II B-M 42.5 N is the safest choice for mass concrete in tropical Bangladesh (lowest ΔT).
Rapid-hardening CEM II A-M 42.5 R behaves closer to Portland cement than to normal composite — requires thermal management in large pours.
VCCTL confirms experimental rankings; over-prediction of blended cements is physically consistent with isothermal vs semi-adiabatic test differences.
2004061
31

## Slide 32
Recommendations For Future Work
1
Extended Material Testing
Test more cement brands & batches; vary w/c (0.30, 0.45, 0.50); investigate elevated curing temperatures relevant to Bangladesh’s tropical climate.
2
Advanced Characterisation
Apply Rietveld XRD for precise phase quantification; combine with XRF elemental analysis; use SEM, TGA & FTIR to characterise hydration products.
3
Scale-Up to Structural Level
Extend from paste to mortar & concrete; study aggregate thermal effects; assess influence of chemical admixtures (retarders, superplasticisers).
4
Thermal Modelling & FEM
Embed Gaussian & polynomial heat models into finite-element solvers; apply Arrhenius activation-energy correction for field temperature prediction.
5
VCCTL Improvement
Supply quantitative phase data, measured PSD and Blaine fineness as inputs; compare isothermal, semi-adiabatic & adiabatic outputs systematically.
6
Field Validation & Guidelines
Monitor temperature in real mass-concrete placements; develop a practical cement-selection guide for temperature-sensitive construction in Bangladesh.
Abdur Nur Tushar • 2004061
Dept. of Civil Engineering, BUET
2004061
32

## Slide 33
Heat of Hydration of Portland and Composite Cements Under Semi-Adiabatic Conditions
Thank You
Abdur Nur Tushar & Zisan Zia
Student No. 2004061 & 2004153
Supervised by
Dr. Raquib Ahsan
Professor, Dept. of Civil Engineering, BUET
Department of Civil Engineering • Bangladesh University of Engineering and Technology • June 2026
Abdur Nur Tushar • 2004061
Dept. of Civil Engineering, BUET
Abdur Nur Tushar • 2004061
Dept. of Civil Engineering, BUET
33